## Slide 1: Rheology of Viscoelastic surfactants and foam in homogeneous porous media
Aarthi Muthuswamy, Clarence Miller, Rafael Verduzco and George Hirasaki
Chemical and Biomolecular Engineering, Rice University
April 23rd, 2012
16th Annual Meeting
Consortium for Processes in Porous Media

## Slide 2: Scope of study
Polymers are very good mobility control agents
Polymers tend to degrade
High shear
High salinity
Presence of divalent ions
High temperature.

## Slide 3: Outline
Aqueous properties of Rhodia’s viscoelastic surfactants
Rheological measurements for viscoelasticity
-Rhodia A in sea water
-Rhodia B in sea water
Foam –experimental set up
Foam measurements(screening tests)
-Foam measurements for Rhodia A
-Foam measurements for Rhodia B
Remarks
Future work

## Slide 4: Outline
Aqueous properties of Rhodia’s viscoelastic surfactants
Rheological measurements for viscoelasticity
-Rhodia A in sea water
-Rhodia B in sea water
Foam –experimental set up
Foam measurements(screening tests)
-Foam measurements for Rhodia A
-Foam measurements for Rhodia B
Remarks
Future work

## Slide 5: Viscosity for 0.3 wt% Rhodia ‘A’ in aqueous solution
Viscosity enhances due to the presence of divalent calcium and magnesium salts
Chart: Steady shear test for Rhodia A 0.3 wt%
| 1 | 1.2589254000000001 | 1.5848932 | 1.9952624000000001 | 2.5118866 | 3.1622778999999999 | 3.9810721999999998 | 5.0118732000000001 | 6.3095746000000004 | 7.9432840000000002 | 10.000002 | 12.589257 | 15.848936 | 19.952629000000002 | 25.118872 | 31.622786999999999 | 39.81073 | 50.118740000000003 | 63.095756999999999 | 79.432854000000006 | 100.00004
Formation brine | 40.8655 | 38.8626 | 36.367 | 33.5218 | 30.8534 | 28.3092 | 26.0013 | 23.8317 | 21.7876 | 19.7831 | 17.8773 | 16.1453 | 14.6306 | 13.4073 | 12.1631 | 11.0498 | 10.0553 | 9.1669 | 8.404 | 7.8759 | 7.4439
sea water | 6.2492 | 6.463 | 6.3735 | 6.4037 | 6.6644 | 6.4871 | 6.3747 | 6.1953 | 5.9952 | 5.8 | 5.5295 | 5.2543 | 4.9634 | 4.6911 | 4.4277
DI water | 2.8794 | 2.9255 | 2.9597 | 2.9105 | 2.8544 | 2.7898

## Slide 6: Appearance of Rhodia ‘B’ 0.3 wt% in DI water after 7 days
Cloudy appearance is noticed.

## Slide 7: Birefringence in Rhodia ‘B’
Original sample
0.3 wt% in DI water after 7 days

## Slide 8: Viscosity for 0.3 wt% Rhodia ‘B’ in aqueous solution
The viscosity is not affected by the presence of divalent salts
Chart: Steady Shear test for Rhodia B for 0.3 wt%
| 0.1 | 0.13894956 | 0.19306978999999999 | 0.2682696 | 0.37275940000000002 | 0.51794748999999995 | 0.71968573000000002 | 1.0000001000000001 | 1.3894956000000001 | 1.9306979 | 2.6826960999999998 | 3.7275941000000001 | 5.1794753 | 7.1968575000000001 | 10.000000999999999 | 13.894957 | 19.306979999999999 | 26.826962000000002 | 37.275944000000003 | 51.794753999999998 | 71.968575000000001 | 100.00001
Formation brine | 120.1282 | 109.5803 | 103.4322 | 90.1152 | 82.3683 | 74.0774 | 65.5306 | 57.8347 | 50.2816 | 42.5914 | 36.5318 | 30.9288 | 26.1674 | 22.1067 | 18.7452 | 15.9229 | 13.6835 | 11.6485 | 9.9869 | 8.6227 | 7.5369 | 6.664
sea water | 144.3873 | 132.183 | 122.9659 | 110.2541 | 96.9347 | 86.5482 | 75.3418 | 64.5768 | 55.7304 | 47.2722 | 39.5902 | 33.4871 | 27.992 | 23.6405 | 19.9412 | 16.7703 | 14.2741 | 12.089 | 10.257 | 8.7427 | 7.5761 | 6.686
DI water | 95.1995 | 76.0577 | 63.2697 | 52.683 | 43.6689 | 36.0465 | 29.3409 | 23.7779 | 19.1244 | 15.2964 | 12.3162 | 9.9401 | 8.1295 | 6.7374 | 5.6922 | 4.8811

## Slide 9: Outline
Aqueous properties of Rhodia’s viscoelastic surfactants
Rheological measurements for viscoelasticity
-Rhodia A in sea water
-Rhodia B in sea water
Foam –experimental set up
Foam measurements(screening tests)
-Foam measurements for Rhodia A
-Foam measurements for Rhodia B
Remarks
Future work

## Slide 10: Phase angle measurement
Courtesy :Introduction to Rheology- Texas Tech University
δ
σ
γ

## Slide 11: Phase angle measurement for elastic and viscous substances
Courtesy :Introduction to Rheology- Texas Tech University

## Slide 12: Phase angle measurement for Viscoelasticity
Courtesy :Introduction to Rheology- Texas Tech University
0°<δ< 90°

## Slide 13: Rhodia ‘A’ 1wt% in sea water
The elastic modulus dominates after a frequency of 8.5 rad/s
Relaxation time is ~0.5 seconds.
Chart: Dynamic frequency test

## Slide 14: Rhodia ‘A’ 1 wt% in sea water- Phase Angle
Chart: Phase Angle for Rhodia A 1 wt% in Sea water
Phase angle measurement lie within 0-90° indicating it is viscoelastic

## Slide 15: Rhodia A 1wt% in sea water- viscosity
Chart: Steady shear test
| 0.1 | 0.12589254999999999 | 0.15848933000000001 | 0.19952624999999999 | 0.25118867 | 0.31622779000000001 | 0.39810719999999999 | 0.50118726000000002 | 0.63095741999999999 | 0.79432833000000003 | 1.0000001000000001 | 1.2589256 | 1.5848935 | 1.9952627000000001 | 2.5118871 | 3.1622786999999999 | 3.9810731000000001 | 5.0118742000000003 | 6.3095759999999999 | 7.9432859000000002 | 10.000005 | 12.589259999999999 | 15.848940000000001 | 19.952632999999999 | 25.118877000000001 | 31.622793000000001 | 39.810738000000001 | 50.118752000000001 | 63.095771999999997 | 79.432868999999997 | 100.00006
Experimental | 274.8761 | 267.064 | 260.8065 | 255.4622 | 246.5131 | 239.3843 | 229.657 | 220.1758 | 210.6031 | 199.4632 | 188.0164 | 177.23 | 165.5201 | 153.8074 | 141.7863 | 129.6346 | 117.8894 | 106.5512 | 95.6924 | 85.5386 | 76.0508 | 67.4286 | 59.3994 | 52.4564 | 46.0042 | 40.2168 | 35.0449 | 30.5878 | 26.7414 | 23.3741 | 20.4727
The zero shear viscosity reaches ~300cP

## Slide 16: Rhodia B 1 wt% in sea water
Elastic modulus dominates throughout the range of study showing how viscoelastic the fluid is
Relaxation time is ~ 3 seconds.
Chart: Dynamic Frequency test for 1 wt% Rhodia B

## Slide 17: Rhodia B 1wt% in sea water- Phase Angle
Chart: Phase Angle for 1 wt% Rhodia B in SW
Phase angle measurement lie within 0-90° showing viscoelastic behavior

## Slide 18: Rhodia B 1 wt% in sea water- viscosity
Zero shear viscosity predicted by the Carreau model gives a value of ~4000cP
Chart: Steady Shear test
| 0.1 | 0.13894956 | 0.19306978999999999 | 0.2682696 | 0.37275940000000002 | 0.51794748999999995 | 0.71968573000000002 | 1.0000001000000001 | 1.3894956000000001 | 1.9306979 | 2.6826960999999998 | 3.7275941000000001 | 5.1794753 | 7.1968575000000001 | 10.000000999999999 | 13.894957 | 19.306979999999999 | 26.826962000000002 | 37.275944000000003 | 51.794753999999998 | 71.968575000000001 | 100.00001
Experimental | 3264.3688 | 2638.0627 | 2095.2976 | 1666.6969 | 1307.7298 | 1019.1935 | 792.1736 | 616.0932 | 480.0941 | 373.5322 | 290.542 | 226.4197 | 176.4705 | 137.4313 | 107.0017 | 83.2349 | 64.985 | 50.4356 | 39.1838 | 30.4372 | 23.7863 | 18.8137

## Slide 19: Outline
Aqueous properties of Rhodia’s viscoelastic surfactants
Rheological measurements for viscoelasticity
-Rhodia A in sea water
-Rhodia B in sea water
Foam –experimental set up
Foam measurements (screening tests)
-Foam measurements for Rhodia A
-Foam measurements for Rhodia B
Remarks
Future work

## Slide 20: Foam experimental set up
Transducer
Transducer
Taps
Taps
Inlet
Nitrogen gas
Co-Injection
Sand: US silica 20-40
Porosity 0.36
Permeability ~80 Darcy
Transducer
Stainless steel sand pack
Syringe Pump
Outlet

## Slide 21: Foam Experiment – Rhodia B
Clean sand US silica 20-40 mesh
Porosity 0.36
Permeability ~ 80 Darcy
Chart: PV liquid injected
Oil injected | 0 | 50
Chart: PV of liquid injected
Oil injected | 0 | 400
Tap 1
6 inch
Tap 2
6 inch
Overall ~24 inch
inlet
outlet
1 wt% in sea water
Foam quality ~83%
Surfactant flow rate 1.2cc/min
Gas flow rate 6 sccm
Tap 1 midpoint 6 inch from inlet
Tap 2 midpoint 12 inch from inlet

## Slide 22: Foam Experiment – Rhodia A
Sand from previous experiment was cleaned and used.
Chart: PV of liquid injected
Chart: PV liquid injected
Tap 1
6 inch
Tap 2
6 inch
Overall ~24 inch
inlet
outlet
1 wt% in sea water
Foam quality ~83%
Surfactant flow rate 1.2cc/min
Gas flow rate 6 sccm

## Slide 23: Effluent of foam generated by Rhodia B

## Slide 24: Remarks
Rhodia B is more viscoelastic at 1wt% in sea water compared to Rhodia A at same conditions.
The zero shear viscosity of Rhodia A ~ 300cP
The zero shear viscosity of Rhodia B ~ 4000cP
Rhodia A and B foam strongly in homogeneous porous media

## Slide 25: Future work
Systematic analysis for the tolerance of these surfactants in the presence of oil.
Conditions under which these surfactants maintain viscoelasticity (temperature, salinity and divalent ion concentration).
Foaming ability of Rhodia viscoelastic surfactants in carbonates using CO2
Foam enhanced oil recovery for high salinity and temperature in cores.

## Slide 26: Acknowledgement
Maura Puerto
Jose Lopez Salinas
Matteo Pasquali
Processes on Porous media consortium
Rhodia

## Slide 27: END

## Slide 28: Backup Slides

## Slide 29: Fit the complex viscosity from Maxwell model – Rhodia A
Chart: Viscosity for 1 wt% Rhodia A in sea water
| 0.1 | 0.12589254999999999 | 0.15848933000000001 | 0.19952624999999999 | 0.25118867 | 0.31622779000000001 | 0.39810719999999999 | 0.50118726000000002 | 0.63095741999999999 | 0.79432833000000003 | 1.0000001000000001 | 1.2589256 | 1.5848935 | 1.9952627000000001 | 2.5118871 | 3.1622786999999999 | 3.9810731000000001 | 5.0118742000000003 | 6.3095759999999999 | 7.9432859000000002 | 10.000005 | 12.589259999999999 | 15.848940000000001 | 19.952632999999999 | 25.118877000000001 | 31.622793000000001 | 39.810738000000001 | 50.118752000000001 | 63.095771999999997 | 79.432868999999997 | 100.00006
Experimental | 274.8761 | 267.064 | 260.8065 | 255.4622 | 246.5131 | 239.3843 | 229.657 | 220.1758 | 210.6031 | 199.4632 | 188.0164 | 177.23 | 165.5201 | 153.8074 | 141.7863 | 129.6346 | 117.8894 | 106.5512 | 95.6924 | 85.5386 | 76.0508 | 67.4286 | 59.3994 | 52.4564 | 46.0042 | 40.2168 | 35.0449 | 30.5878 | 26.7414 | 23.3741 | 20.4727
Complex viscosity | 222.9516 | 224.8839 | 227.2214 | 230.0086 | 233.2641 | 236.9498 | 240.9223 | 244.8601 | 248.1714 | 249.9116 | 248.7924 | 243.4097 | 232.769 | 216.9339 | 197.3072 | 176.1682 | 155.7389 | 137.4561 | 121.8178 | 108.6564 | 97.5257 | 87.98 | 79.6582 | 72.2206 | 65.2748 | 58.4083 | 51.3348 | 44.0431 | 36.807 | 30.0282 | 24.0388

## Slide 30: Fit the complex viscosity from Maxwell model – Rhodia B
Chart: Viscosity of rhodia B 1 wt% in Sea water
| 0.1 | 0.13894956 | 0.19306978999999999 | 0.2682696 | 0.37275940000000002 | 0.51794748999999995 | 0.71968573000000002 | 1.0000001000000001 | 1.3894956000000001 | 1.9306979 | 2.6826960999999998 | 3.7275941000000001 | 5.1794753 | 7.1968575000000001 | 10.000000999999999 | 13.894957 | 19.306979999999999 | 26.826962000000002 | 37.275944000000003 | 51.794753999999998 | 71.968575000000001 | 100.00001
Experimental | 3264.3688 | 2638.0627 | 2095.2976 | 1666.6969 | 1307.7298 | 1019.1935 | 792.1736 | 616.0932 | 480.0941 | 373.5322 | 290.542 | 226.4197 | 176.4705 | 137.4313 | 107.0017 | 83.2349 | 64.985 | 50.4356 | 39.1838 | 30.4372 | 23.7863 | 18.8137
Complex viscosity | 2625.3009 | 2529.966 | 2371.9723 | 2135.6662 | 1827.7527 | 1484.4457 | 1153.5969 | 869.0885 | 642.5846 | 470.6425 | 343.8223 | 252.0434 | 186.6533 | 140.7909 | 109.0578 | 87.0241 | 70.9471 | 57.9526 | 46.4592 | 36.165 | 27.3701 | 20.2882

## Slide 31: Ratio of pressure drops for Rhodia A and B
Rhodia B
Chart: PV of liquid injected
Rhodia A
Chart: PV liquid injected

## Slide 32: Rhodia B effluent foam in the presence of oil