## Slide 1: Bottlebrush Polymer & Surfactant Blends for Low IFT
Luqing Qi, Hadi ShamsiJazeyi, Xianyu Li, Stacy Pesek, Maura Puerto, Rafael Verduzco, George Hirasaki
Department of Chemical and Biomolecular Engineering
Rice University, Houston, TX, 77005

## Slide 2: Background
The phase behavior of surfactant and surfactant blends can be analyzed through salinity scans
The phase behavior goes from Winsor Type I to Winsor TypeⅡwith the increase in salinity. A bicontinuous middle phase may result in ultralow interfacial tension (IFT) values

## Slide 3: Polymer additives can influence phase behavior and micelle structure
R. Nagarajan, J. Chem. Phys. 90 (3), 1 February 1989
What will happen to phase behavior, interfacial tension(IFT) and CMC if we add polymers or polymer coated nanoparticles into this system?
Hydrophilic chain
Hydrophobic chain

## Slide 4: Bottlebrush polymers: densely grafted branched polymers
Matyjaszewski et al., Macromolecules 2001

## Slide 5: Synthesis of bottlebrush polymer
●Norbornenyl-chain transfer agent (NB-CTA)
● Reversible addition fragmentation chain-transfer (RAFT) synthesis of side-chain
● Ring-opening metathesis polymerization (ROMP) to make bottlebrush polymer
● Removal of terminal CTA through aminolysis
Provides control over bottlebrush side-chain and backbone length
Li, Verduzco et al., Soft Matter 2014, 10, 2008-2015.

## Slide 6: PNIPAAM is thermoresponsive and exhibits an LCST
PNIPAAM
T < 32oC
T > 32oC
without CTA
with CTA
PolyNIPAAM Bottlebrush Polymers exhibit an LCST near 32 oC
Side-chain length | 4K | 5.6K | 9K
with CTA | 25.52°C | 29.75°C | 30.25°C
without CTA | 31.76°C | 34.25°C | 34.30°C
PNIPAAM is water soluble at room temperature, insoluble above 32 oC
Notes: PNIPAAM is water soluble at room temperature, insoluble above 32 oC

## Slide 7: PNIPAAM bottlebrushes exhibit a modest decrease in oil/water IFT
PNIPAAM Bottlebrush polymer

## Slide 8: Bottlebrush Polymer
Poly(N-isopropyl acrylamide)
(PNIPAAM) bottlebrush
 | MW (g/mol) |  | PDI |  | Side chain MW (g/mol)
PNIPAAM bottlebrush | 2.8×105 |  | 1.11 |  | 7000 (40 per bottlebrush)
PEG bottlebrush | 1.0 ×106 |  | 1.28 |  | 5000 (200 per bottlebrush)
Poly(ethylene glycol)
(PEG) bottlebrush

## Slide 9: Analysis of surfactant/bottlebrush polymer blends
Surfactant: C12 4,5 orthoxylene sulfonate(OXS)
Analyze the phase behavior and oil-water interfacial tension of:
●OXS surfactant
●OXS surfactant and PNIPAAM bottlebrush polymer blend
●OXS surfactant and PEG bottlebrush polymer blend
Surfactant provided by ExxonMobil
Active sodium sulfonate 82.5%
PNIPAAM Bottlebrush polymer
Notes: Exam pure surfactant, nb, blend compare ift phase behavior

## Slide 10: OXS Phase Behavior
From salinity scan, the optimal salinity for pure OXS surfactant is around 1.7wt%
1.4 %
2.4 %
Salinity scan of pure OXS
2% Surfactant, 2.5% alcohol, 1mL octane, 1.4%-2.4%NaCl
Optimal salinity around 1.7wt%

## Slide 11: OXS + Bottlebrush phase behavior
Salinity scan of OXS surfactant-PNIPAM bottlebrush
2% Surfactant, 2.5% alcohol, 1mL octane, 0.1 % bottlebrush, 1.4%-2.4%NaCl
Optimal salinity around 1.9wt%
From salinity scan, the optimal salinity for pure OXS surfactant-PNIPAM bottlebrush blend is around 1.7wt%
1.4 %
2.4 %

## Slide 12: Interfacial Tension (IFT) Measurement
IFT measurement is done through spinning drop tensiometer (Grace Instruments M6500)
Mobile
phase
Stationary
phase
Range of measurement
Range of spinning rate:
0 11000 rpm
Where
= the difference in specific gravity of the two phases in g/
=diameter of drop in mm
= spinning rate in rpm
Notes: 10-6

## Slide 13: IFT Comparison Shows Synergistic Interaction
At optimal salinity, measurements were sampled from upper and lower phases. All other measurements were sampled from microemulsion.
System | NaCl concentration | IFT (mN/m)
Pure surfactant | 1.4 % 1.7 % (optimal) | 2.23×10-2 2.76×10-2
 | 2.0 % | 5.46×10-2
Surfactant + 0.1 % PNIPAAM Bottlebrush | 1.4 % | 3.67×10-2
 | 1.5 % 1.9% (optimal) | 5.46×10-2 7.52×10-3
 | 2.0 % | 2.78×10-4
Surfactant + 0.1 % PEG Bottlebrush | 1.4 % | 4.69×10-2
 | 2.0 % | 3.78×10-4
Notes: Add optimal salinity here specify upper phase

## Slide 14: Hypothesis: surfactant/polymer associations
Associations between polymer and surfactant result in a shift in the phase behavior and decrease in the IFT
Associations can increase the CMC
Notes: General , affect CMC

## Slide 15: Conclusions: Bottlerush- Surfactant Hybrids
  ●Bottlebrush polymers give only a modest reduction in oil/water IFT.
  ●Blends of bottlebrush polymers with surfactant result in significant changes to the surfactant phase behavior and a decrease in the IFT at optimal salinities
  ●Small amount of bottlebrush polymer additive (0.1wt %) produces significant reductions in IFT
Notes: 15

## Slide 16
  Measure the critical micelle concentration (CMC) of bottlebrush/surfactant blends
  Characterize surfactant-bottlebrush associations through dynamic light scattering, X-ray scattering, and electron microscopy
  Analyze the rheological properties of bottlebrush polymer/surfactant blends
  Future Work

## Slide 17
Thanks for your attention!
Question?
The authors acknowledge the financial support from Rice University Consortium for Processes in Porous Media

## Slide 18: Backup slides

## Slide 19: OXS + linear PNIPAAM phase behavior
Salinity scan of OXS surfactant-PNIPAM linear polymer
2% Surfactant, 2.5% alcohol, 1mL octane, 0.1 % polymer, 1.4%-2.0%NaCl
Optimal salinity over 1.9wt%
From salinity scan, the optimal salinity for pure OXS surfactant-PNIPAM linear macromonomer blend is around 1.7wt%
1.4 %
2.4 %