## Slide 1: Asphaltene Deposition in Microfluidic System
Yu-Jiun Lin (Nate), Mohammad Tavakkoli, Francisco M. Vargas, Sibani Lisa Biswal
2014.04.21

## Slide 2
*Jill Buckley’s Lab (New Mexico Tech)
n-C5 Asphaltene
n-C7 Asphaltene
Polydisperse distribution
Precipitate due to Pressure, Temperature, and composition
(Oil industry)
What is Asphaltene?
Notes: Asphaltene is polydisperse in crude oil
Typical looking of C5 and C7 asphaltene
C5 means the precipitant is n-pentane, and C7 is n-heptane

## Slide 3
Soluble: aromatics (toluene and xylene)
Insoluble: n-alkane (n-heptane and n-pentane)
*O. C. Mullins et al, Energy&Fuels, 2012
Yen-Mullins Model
Asphaltene Stages
Irreversible deposition
(Aging effect)
Notes: What is asphaltene? Asphaltene is brownish, black, sticky, and the heaviest part of the crude oil.
In general, asphaltene is defined as a fraction of crude oil insoluble in excess normal alkanes, such as n-pentane or n-heptane but soluble in benzene or toluene
As you can see, this picture is the Yen-Mullins Model, it describes hierarchy of the asphaltene

## Slide 4
Syringe Pump
Computer
Microscope
Micro-channel
T-junction
Precipitant
Crude oil
Pressure Transducer
Sample Collection
for viscosity measurement
Vial
Vial
Experimental Setup

## Slide 5
Syringe Pump
Inverted Microscope
Micro-channel
T-junction
Pressure
Transducer
Precipitant
Crude oil
Vial
Experimental Setup

## Slide 6
Use transparent, organic resistant, and porous media design
*J. Wang et al, J. Disp. Sci. &Tech., 2004
*E. S. Boek et al, Energy&Fuels, 2008
50μm
500μm
Glass capillary tube-> not easy to design a complex pattern and size is too big
Stainless steel -> not transparent
PDMS->not organic resistant
*K. Ma et al, Soft Matter, 2012
Previous Work

## Slide 7
n-C7 78.4%, Oil 21.6%
20 Celcius
Centrifuged oil
60 μl/min
Asphaltene : 0.21 wt%
125μm
H : 20 μm
Real-time Asphaltene Deposition
22μm
Notes: Reduce the porosity and permeability

## Slide 8
Chart: Asphaltene deposition
| 60 | 120 | 240 | 360 | 480 | 600 | 720 | 840 | 1080 | 1200 | 1320 | 1380 | 1440 | 1560
 | 4.3991 | 5.9212 | 13.1893 | 19.8798 | 49.4439 | 59.6446 | 66.1876 | 71.5425 | 75.5935 | 83.6837 | 86.8832 | 93.7285 | 95.8322 | 98.7358
Chart: Pressure Drop
Chart: Permeability Reduction
Imaging Process
Pressure transducer
Calculation
Homogeneous micromodel
Permeability Reduction

## Slide 9
Aging Effect
Aging time : 0 hr
Aging time : 144 hr
Original picture (Before washing)
Solubility parameter for mixture:
∅i : volume fraction
i : solubility parameter for pure substance

## Slide 10
The higher the instability,
the more soluble asphaltene
will precipitate out.
Instability for Aging
Aging time : 72 hrs
(δonset – δmixture90)
(δonset – δmixture72)
(δonset – δmixture50)
Instability: (δonset – δmixture)

## Slide 11
Chart: Amount of precipitated asphaltene
| 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90
 | 0.45833 | 0.33333 | 1.1111 | 2.4667 | 4 | 4.5556 | 5 | 5
Chart: Injected Precipitated Asphaltene (mg)
| 0.44159999999999999
20% C7 | 0.11791
30% C7 | 4.9274 | 5.3056 | 5.602 | 6.3883 | 6.64 | 7.5363 | 8.0363 | 8.2602
40% C7 | 8.7075 | 9.9779 | 11.9365 | 15.911 | 19.1395 | 20.5272 | 26.3702 | 28.1984 | 30.3418 | 34.021
50% C7 | 8.5431 | 14.5689 | 19.3152 | 26.2446 | 30.1811 | 38.8356 | 45.6139 | 51.7112 | 52.627 | 56.9943
60% C7 | 6.5612 | 12.394 | 28.161 | 44.6899 | 52.6083 | 63.3787 | 77.0935 | 82.1871 | 85.3821
70% C7 | 11.2863 | 18.6117 | 30.0261 | 41.3163 | 58.7608 | 59.6446 | 66.1876 | 72.5405 | 79.2421 | 79.7109 | 85.6451
80% C7 | 13.9495 | 20.767 | 41.1973 | 48.8481 | 66.2381 | 70.7676 | 86.0913 | 89.5113 | 93.2319 | 95.6939
90% C7 | 13.1621 | 13.7058 | 13.9303 | 26.2092 | 43.4609 | 52.9932 | 60.3413 | 68.4127 | 72.5527 | 75.2347
Instability for Deposition
Ratio of nC7
Instability: (δonset – δmixture)

## Slide 12
Before washing
Washing Effect

## Slide 13
After 67%heptane and 33% toluene washed (Poor solvent)
Before washing
Washed by poor solvent
Increased light intensity from the original imaging by 70%
Confocal Laser Scanning
Washing enhanced the aging effect
Dissolved asphaltenes
and resins

## Slide 14
Organic resistant microfluidic channels are able to provide real time asphaltene deposition with permeability reduction.
With high sensitivity micromodels, aging and washing effects can be analyzed.
A criteria for the instability of aging effect and deposition is proposed.
Conclusion

## Slide 15
Acknowledgement
This work was financially supported by
ADNOC

## Slide 16
Thank you

## Slide 17
The fluorescence is coming from both resins and dissolved asphaltenes.
By adding heptane to the mixture, asphaltenes start to aggregate and these
asphaltene aggregtaes are not fluorescent.
Model oil: C7+ Asph.+Toluene
Model oil + Heptane
Aggregate Fluorescence

## Slide 18
C7+ dilute 40x
Chart: Emission Curve (excitation 410nm)
Excitation wavelength for confocal laser scanning

## Slide 19
Chart: Emission Curve (excitation 488nm)
C7+ dilute 40x
Excitation wavelength for confocal laser scanning

## Slide 20
C7+ dilute 40x
Chart: Emission Curve (excitation 580nm)