## Slide 1
Nanoparticle Interactions with Surfactant Micro-emulsions
19th Annual Meeting of
Rice University Consortium for Process in Porous Media
April 22, 2015
Luqing Qi,1 Hadi ShamsiJazeyi,1 Jason Mann,2 Maura Puerto,1 James M. Tour,2 Rafael Verduzco,1 George J. Hirasaki1
1Department of Chemical and Biomolecular Engineering
2Department of Chemistry

## Slide 2: Goal
● Prepare and characterize nanoparticles (NPs) that can segregate to the middle phase microemulsion at high salinities and penetrate porous media
● Investigate the interaction of nanoparticles with surfactants towards an approach to prepare blends with low interfacial tension (IFT) and low adsorption

## Slide 3: Prior studies have shown NPs stabilize macro-emulsions
“unmodified nanoparticles …..show improved stability of large emulsion droplets”1
“Emulsions have been stabilized by carbon nanotube-silica nanohybrids. “
1. B. P. Binks, Curr. Opin. Colloid Interface Sci., 2002, 7, 21–41.
2. M. Shen, D. E. Resasco, Langmuir 2009, 25(18), 10843–10851

## Slide 4: Nanoparticles that stabilize bicontinuous microemulsions could be beneficial for EOR
Reed and Healv (1976, June 1). Multiphase Microemulsion Systems. SPE jounals.
As salinity increases, Winsor typeⅠ to
Winsor type Ⅲ, then to Winsor type Ⅱ
Microemulsion is a bicontinuous phase

## Slide 5: Preparation of NPs: Surface modification of oxidized carbon black
Oxided Carbon black
sPVA: Lightly sulfated PVA
ssPVA: Highly sulfated PVA
hydrophobic
hydrophilic

## Slide 6: Library of NPs with amphiphilic polymer chains on the surface
sPVA—more Hydrophilic chain
ssPVA--most Hydrophilic chain
The amphiphilicity is the balance between alkyl group and sulfate group
The degree of sulfation can be controlled
C16--Hydrophobic chain
PVA—more Hydrophilic chain
sPVA: Lightly sulfonated PVA
ssPVA: Highly sulfonated PVA
Oxided Carbon black
C16PVA-OCB
C16sPVA-OCB
C16ssPVA-OCB
ssPVA-OCB
PVA-OCB
sPVA-OCB

## Slide 7: Amphiphilic nanoparticles are surface active
K3: Cn(n<14) propoxy ethoxy sulfates
Nanoparticle: C16 sPVA-OCB
CMC of K2 surfactant
Measured using Wilhelmy plate method,
Kruss K100 tensiometer

## Slide 8: No microemulsion observed from salinity scan of nanoparticle
Oil phase: n-octane
No surfactant was used
NP: 2mg/g partially sulfated poly(vinyl alcohol)-OCB ("sPVA-OCB")
Pickering emulsion:
a macro-emulsion stabilized by solid particles adsorbed onto the interface between the two phases.
Pickering emulsion observed in a salinity scan: flat interface, emulsion is kinetically stable
Salinity %
0.0 5.3 6.4 7.6 9.9 10.5 11.4 14.7 16.0

## Slide 9: Surfactant-Nanoparticle blends can potentiall produce stable microemulsions
S13B
From TIORCO
Alfoterra K2-4 1S and Alfoterra K3-4 1S
From Sasol
Cn(n<14) propoxy ethoxy sulfates
K2 and K3 have same PO,EO number,
K3 has long hydrophobe part
OXS from Exxon
Salinity scan of surfactant first, then surfactant& NPs blend

## Slide 10: Salinity scan for S13B surfactant
Salinity % 3.0 3.5 4.0 4.5 5.0 5.5 6.0 6.5 7.0 7.5 8.0
1cc Aqueous: S13B 2wt%, SBA 2.5wt%
1cc oil: octane
the optimal salinity between 4.0~4.5%

## Slide 11: PVA-OCB does not penetrate into microemulsion phase
1cc Aqueous: S13B 2wt%, Nacl 4.3wt%, PVA-OCB 0.2wt%
1cc oil: octane
SBA % 3.0 3.5 4.0 4.5 5.0 2.5 3.0 3.5 4.0 4.5 5.0
without OCB
with PVA-OCB

## Slide 12: C16sPVA-OCB disperses in microemulsion, but aggregate with time
1cc Aqueous: S13B 2wt%, Nacl 4.3wt%, OCB 2wt%
1cc oil: octane
sPVA-OCB C16PVA-OCB C16sPVA-OCB
SBA% 3.0 5.0 3.0 5.0 3.0 5.0
Aggregate after
a few days

## Slide 13: Highly sulfated C16ssPVA-OCB NPs are stable in microemulsion
1cc Aqueous:C16ssPVA-OCB 0.2wt%, S13B 2wt%, SBA 5wt%
1cc oil: octane
Salinity % 3.3 3.5 3.7 3.9 4.1 4.3 4.5 3.3 3.5 3.7 3.9 4.1 4.3 4.5
Homogeneous dispersion
S13B 4.3% optimal salinity

## Slide 14: Highly sulfated NPs are stable in microemulsions at various salinities: OXS surfactant + NP
S13B 4.3% optimal salinity
Salinity %
1.5 1.6 1.7 1.8 1.9 2.0
optimal salinity ~1.6%
1.4 1.6 1.7 1.8 1.9 2.0 2.1 2.2 2.3 2.4
OXS 1.6% optimal salinity
1cc Aqueous: OXS 2wt%, SBA 2.5wt%, C16ssPVA-OCB 0.2wt%,
1cc oil: octane

## Slide 15: Highly sulfated NPs are stable in microemulsions at various salinities: AF-K3-4 surfactant + NP
Salinity %
9.5 9.7 9.9 10.1 10.3 10.5 11.0 11.5 12.0 12.5 13.0 11.0 11.2 11.4 11.6 11.8 12.0 12.2 12.4 12.6 12.8 13.0
1cc Aqueous: AF K3-4 1S 4wt%, SBA 2.5wt%, C16ssPVA-OCB 2%
1cc oil: octane
S13B 4.3% optimal salinity
OXS 1.6% optimal salinity
K3 11.9% optimal salinity

## Slide 16: Alfoterra K2-15 surfactant exhibits an optimal salinity near 15 %
Salinity %
14.0 14.2 14.4 14.6 14.8 15.0 15.2 15.4 15.6 15.8 16.0 14.0 14.2 14.4 14.6 14.8 15.0 15.2 15.4 15.6 15.8 16.0
1cc Aqueous: AF K2-4 1S 4wt%, SBA 2.5wt%
1cc oil: octane
Optimal salinity between 15.2~15.4 %
S13B 4.3% optimal salinity
OXS 1.6% optimal salinity
K3 11.9% optimal salinity

## Slide 17: C16ssPVA-OCB disperses in K2 microemulsion at 15 % salinities
OXS 1.6% optimal salinity
S13B 4.3% optimal salinity
K3 11.9% optimal salinity
1cc Aqueous: AF K2-4 1S 4wt%, SBA 2.5wt%, C16ssPVA-OCB 2%
1cc oil: octane
Salinity %
14.0 14.2 14.4 14.6 14.8 15.0 15.2 15.4 15.6 15.8 16.0 14.0 14.2 14.4 14.6 14.8 15.0 15.2 15.4 15.6 15.8 16.0
K2 15.2% optimal salinity

## Slide 18: C16ssPVA-OCB stays stable at high salinity microemulsions after a week
Salinity %
14.0 14.2 14.4 14.6 14.8 15.0 15.2 15.4 15.6 15.8 16.0 14.0 14.2 14.4 14.6 14.8 15.0 15.2 15.4 15.6 15.8 16.0
1cc Aqueous: AF K2-4 1S 4wt%, SBA 2.5wt%, C16ssPVA-OCB 2%
1cc oil: octane
After a week, 15.0~15.2% stays stable, 15.4~16.0% precipitates severely. i.e. at salinity a little higher than optimal, less water in microemulsion, and C16ssPVA-OCB more easily precipitates out

## Slide 19: NPs disperse in surfactant microemulsion at all salinities tested
ssPVA--most Hydrophilic chain
C16--Hydrophobic chain
The amphiphilic C16ssPVA-OCB disperses and stay stable in microemulsion from low salinity to ultra high salinity
Cn(n<14) propoxy ethoxy sulfates
K2 and K3 have same PO,EO number,
K3 has long hydrophobe part
OXS 1.6% optimal salinity
S13B 4.3% optimal salinity
K3 11.9% optimal salinity
K2 15.2% optimal salinity

## Slide 20: Small-angle X-ray scattering(SAXS) provides measure of domain size
https://www.sni-portal.de/kfs/Methoden/smallanglescattering.php
T. Sottmann, R. Strey, and S.-H. Chen
J. Chem. Phys. 106, 6483 (1997)

## Slide 21: SAXS measurement reveals a small increase in domain size with NPs present
Experiment done in Argonne national lab
K3: Cn(n<14) propoxy ethoxy sulfates
Nanoparticle: C16ssPVA-OCB
q(Å)
Domain size ≈44nm
Domain size ≈48nm

## Slide 22: SAXS measurements show a small decrease in domain size for K2 microemulsion
K2: Cn(n<14) propoxy ethoxy sulfates
Nanoparticle: C16ssPVA-OCB
q(Å)
Experiment done in Argonne national lab
0.02Å
Domain size ≈31nm

## Slide 23: Domain size is relatively insensitive to the presence of NPs
Domain size of octane-water-surfactant microemulsion is comparable with the size of NPs ( diameter is roufhly 50 - 100nm)
With addition of NPs, no significant change in domain size
30~50nm

## Slide 24: Breakthrough Studies in Sandstone Column
More than 95% of LsPVA-OCB can flow through sandstone column at 70 ºc in API brine
sPVA(50 K)-OCB was dispersed in API brine (8 wt% NaCl, 2 wt% CaCl2)
The concentration of nanoparticles was 20 mg/L
Flow rate is 8 mL/h (linear velocity 12.2 m/d)

## Slide 25: Future work
Inject the NPs and surfactant blend into core (epoxy sealed Berea core ready), and test the adsorption of surfactant w/o Nps
2. Analyze the micro-structure of NPs-surfactant microemulsion by cryo-TEM measurements
Y. Y. Won, A.K. Brannan, H. T. Davis, F. S. Bates
J. Phys. Chem. B 2002, 106, 3354-3364

## Slide 26: Summary
We can prepare amphiphilic nanoparticles through modificaiton of oxidized carbon black
The amphiphilicity of the nanoparticle can be adjusted by the composition of the polymers attached to the surface.
Highly sulfated nanoparticles are found to be most stable and able to penetrate bicontinuous microemulsion phases.
SAXS measurements show that the NPs do not significantly change the domain size for the bicontinuous microemulsion.

## Slide 27
The authors acknowledge the financial support from Rice University Consortium for Processes in Porous Media and Advanced Energy Consortium(AEC).
This research used resources of the Advanced Photon Source, a U.S. Department of Energy (DOE) Office of Science User Facility operated for the DOE Office of Science by Argonne National Laboratory under Contract No. DE-AC02-06CH11357.

## Slide 28: Backup slides
Sample Name | Average Diameter (nm)
PVA_OCB_10k | 61
PVA_OCB_10ks | 38
PVA_OCB_10kss | 215
PVA_OCB_6k | 43
PVA_OCB_6ks | 63
PVA_OCB_6kss | 240
PVA_OCB_2k | 54
PVA_OCB_2ks | 170
C16PVA_OCB_2k | 72
C16PVA_OCB_2ks | 151
C16PVA_OCB_2kss | 123
Dynamic light scatterring(DLS)

## Slide 29: Backup slides
Thermogravimetric Analysis (TGA)
number | type | Weight added | At 200℃ | At 600℃ | Polymer fraction
1 | 2k PVA-OCB | 14.4280mg | 86.0% | 9.0% | 89.53%
2 | sPVA-OCB | 12.5300mg | 79.5% | 17.5% | 77.99%
3 | C16-PVA-OCB | 14.9840mg | 96.0% | 9.0% | 90.63%
4 | 16k sPVA-OCB | 15.4390mg | 94.0% | 5.7% | 93.94%
5 | C16-ssPVA-OCB | 14.2190mg | 83.0% | 24.5% | 70.48%
6 | 6k sPVA-OCB | 8.0760mg | 95.0% | 12.0% | 87.37%
7 | 6k PVA-OCB | 18.7910mg | 64.0% | 2.5% | 96.09%
8 | C16-sPVA-OCB | 9.3870mg | 96.0% | 2.6% | 97.29%
9 | 10k PVA-OCB | 23.5380mg | 43.7% | 2.0% | 95.42%
10 | 10k ssPVA-OCB | 2.1390mg | 80.0% | 50.5% | 36.88%
11 | 10k ssPVA-OCB |  |  |  | 
12 | 6k ssPVA-OCB | 10.6790mg | 72.5% | 14.9% | 79.45%
13 | 6k ssPVA-OCB | 1.4610mg | 79.9% | 2.5% | 96.87%

## Slide 30
TGA curve
C16PVA-OCB