## Slide 1: Asphaltene Aggregation and Deposition in Porous Micromodel
Yu-Jiun “Nate” Lin
Peng He, Mohammad Tavakkoli, Francisco M. Vargas, Sibani Lisa Biswal
April 2015
Biswal Research Group

## Slide 2
*Oilfield review, Summer 2007
Solids in subsea flow line
Solids built up
in wellbore
Asphaltene deposition
in near-wellbore region
Types of Asphaltene Problems
Plugging
W/O Emulsion
Solids in separators
*L. Alvarez et al., Fuel, 2010
Notes: Asphaltene deposition in pipelines and oil reservoirs has resulted in a great amount of devastating problems by reducing well productivity since decades ago.
As you can see, this figure illustrates asphaltene can deposit in different parts of oil production facilities, which are the separator, flow lines, wellbore, and near-wellbore region.
We need full understanding about the mechanism of asphaltene deposition to prevent these problems.
Moreover, asphaltene-stabilized water-in-oil emulsions cause fluids in oil production process to be highly viscous, which increases the costs for transportation. These stable emulsions make separation of water and oil for high quality of oil very difficult.

## Slide 3
*SPE Distinguished Lecturer Program
Worldwide Asphaltene Problem
Venezuela
North Sea
Canada
Middle East
Gulf of Mexico
Asphaltene deposition problems to date are confined to specific areas and relatively light fluids, however :
Increased focus on the EOR unravels new potential challenges in the area of precipitation/deposition of previously “ stable” hydrocarbon fluids.
High cost of remediation:
~ $500 k/well onshore
~ $3 MM/well offshore

## Slide 4
*Jill Buckley’s Lab (New Mexico Tech)
n-C5 asphaltene
n-C7 asphaltene
Polydisperse distribution, a global asphaltene molecule does NOT exist
Precipitate due to pressure, temperature, and composition change
Insoluble: n-alkane (n-heptane and n-pentane)
Soluble: aromatics (toluene and xylene)
(Oil industry)
What is Asphaltene?
Precipitation -> simulation tools by Dr. Vargas (simplified equation for deposition)
Deposition -> needs more experiments -> microfluidic devices
*J. Creek, EnergyFuels, 2013
Notes: What is asphaltene? Asphaltene is brownish, black, strong self-associating, and the heaviest part of the crude oil.
In general, asphaltene is defined as a fraction of crude oil insoluble in excess normal alkanes, such as n-pentane or n-heptane but soluble in benzene or toluene
Typical looking of C5 and C7 asphaltene , C5 is more powder-like and C7 is more crystal-like
C5 means the precipitant is n-pentane, and C7 is n-heptane

## Slide 5
Organic-resistant NOA81 Microchannel
Reduced reagent consumption
Lab on a chip (mixing, heating, separation, reaction)
Compatible with crude oils and toluene
Reusable and transparent
Wide temperature range (-150oC ~ 125oC)
Easy to adjust the surface properties
*L.-H. Hung et al., Lab Chip, 8, 983–987, 983, 2008
*N.H.G. Rahmani et al., SPE 121414, 2009
Deposition is detected both macroscopically (pressure drop) and in the pore scale (visualization).
BLACK BOX
(core flooding)
500µm
* Yu-Jiun Lin et al. Lab on a Chip, in preparation 2015

## Slide 6
Syringe pump
Computer
Microscope
Micro-channel
T-junction
Precipitant
Oil
Pressure transducer
Sample collection
for viscosity measurement
Vial
Vial
Schematic Experimental Setup
Change composition
T and P are constants
Fixed length for constant aggregation time (100s)
* Yu-Jiun Lin et al. Lab on a Chip, in preparation 2015
Notes: 20 font

## Slide 7
Visualization of Asphaltene Deposition
600µm
25µm
Deposition time: 10 mins
Flow direction
Notes: 20 font

## Slide 8
Bulk - Deposition Potential
Fractal
Chunk
Spherical
By mixing n-heptane with model oil, aggregates will change into three phases (spherical, fractal, chunk), and these aggregates will change behaviors of deposition.
* Yu-Jiun Lin et al. Lab on a Chip, in preparation 2015
250µm
250µm
250µm
(1) 40 - 50 vol%
(2) 55 – 60 vol%
(3) 65 – 80 vol%
5µm
5µm
30µm
Notes: We have known that ….
In the figure, for 40-50% of heptane, spherical aggregates are small enough to be carried by fluids with a very low deposition rate
For 55-60%, the fractal aggregates start to form and enhance the deposition rate
After 65%, the chunk aggregates appear, and they cause the bridging effect

## Slide 9
Bulk - Prediction Model
* Yu-Jiun Lin et al. Lab on a Chip, in preparation 2015
Particle collection model for the fibrous filter (near-wellbore region) -> both size and concentration of particles
With this capability, we can analyze and predict the ability of dispersants
Notes: After obtaining the size and particle concentration, the particle collection model … is utilized

## Slide 10
Dispersant + 0.5wt% Model Oil
100 ppm dispersant X
No dispersant
* Yu-Jiun Lin et al. EnergyFuels, in preparation 2015
Mixing 100 ppm of dispersant X, Y, and octylphenol (resin-like molecule) changes the aggregation morphology significantly.
By obtaining the size and the concentration of these particles, the capture efficiency can be calculated.
100 ppm octylphenol
100 ppm dispersant Y
 | Radius (µm)
Dispersant X | 13.55
Octylphenol | 14.12
Dispersant Y | 25.04
No dispersant | 49.51
Notes: Three dispersants are chosen, dispersant X, Y, and octylphenol
The sizes are obtained by microscopic analysis.

## Slide 11
Dispersant + 0.5wt% Model Oil
100 ppm dispersant X
No dispersant
500 μm
500 μm
100 ppm dispersant Y
500 μm
Deposition patterns are also changed by adding dispersants
Dispersant X : stronger dispersant
Dispersant Y : weaker dispersant
Only aggregation morphology is affected by dispersants, but not precipitation.
* Yu-Jiun Lin et al. EnergyFuels, in preparation 2015
Notes: Flow tests also show that the deposition rate is highly dependent on the particle size

## Slide 12
Deposition Rate
* Yu-Jiun Lin et al. EnergyFuels, in preparation 2015
Deposition rate: Octylphenol ~ Dispersant X > No dispersant > Dispersant Y
Size: No dispersant > Dispersant Y > Octylphenol ~ Dispersant X
Because of identical amounts of precipitation, smaller size means higher particle concentration
Chart: 
Notes: After image processing, we can find that octylphenol and dispersant X have the same deposition rate because of similar particle size
With high particle concentration, dispersant X and octylphenol have the highest deposition rate
Aggregates are large without dispersant, so the impaction by the inertia dominates. Therefore, dispersant Y has the lowest deposition rate.

## Slide 13
Chart: Normalized Efficiency
Dispersant X | 0.94165
Dispersant X | 1
 | 0
Dispersant Y | 0.415
Y | 0.325
 | 0
Octylphenol | 1
C8 | 0.90417
 | 0
No dispersant | 0.47157
no | 0.54167
Deposition Rate and Capture Efficiency
* Yu-Jiun Lin et al. EnergyFuels, in preparation 2015
Using the particle size from microscopy and particle concentration from absorbance, the efficiencies can be acquired by the collector model. Results from experiments and theory are qualitatively consistent.
Theoretical
Experimental
Dispersant X
Dispersant Y
Octylphenol
No dispersant
Notes: The black column represents results from theory, and the white ones are from experiments.

## Slide 14
Pore-scale Interstitial Velocity Simulation
* Done by Dr. Peng He
With the ability to visualize real time deposition, the video can be used to simulate the interstitial velocity profile, and calculate the drag forces.
Drag forces are higher in red areas, which matches the deposition patterns.
Simulation
Experiment
* Yu-Jiun Lin et al. EnergyFuels, in preparation 2015
Beginning
Beginning
10 mins
10 mins

## Slide 15
Conclusion
Organic-resistant microfluidic devices are fabricated for visualizing real-time asphaltene deposition processes.
A capture efficiency model successfully predicts the potential of asphaltene deposition by two parameters, size and concentration, consistent with the results from pressure drop measurements and deposition rate.

## Slide 16
Acknowledgements
Supported by

## Slide 18
Pore-scale Particle-surface Interaction
* G. Ziskind, Reviews in Chemical Enigneering, 2006
: Hamaker constant
In the pore scale, a combination of drag force and adhesion force acting on a particle can be estimated to analyze the deposition rate.
* Goldman et al. (1967) and O’Neill (1968)
* Doris Gonzalez et al. PhD thesis, Rice University 2008
Notes: In addition to the capture efficiency calculated macroscopically, we can also analyze the particle-surface interaction in the pore scale
As

## Slide 19
Pore-scale - Hamaker Constant (vdW)
Asphaltene
80 vol% Heptane + 20 vol% Toluene
NOA 81 + Asphaltene thin layer
Asphaltene
2
A132 Sticking Tendency
Hamaker constant : a material property that represents the strength of van der Waals interactions between macroscopic bodies
* Doris Gonzalez et al. PhD thesis, Rice University 2008
3- Lean phase
2- Rich phase
1- Substrate
 | A132(x1020J)
No dispersant | 0.051
Dispersant X | 0.002
steric repulsion

## Slide 20
With addition of dispersant X, the deposition rate of asphaltenes from the crude oil increases
Dispersant X+ Crude Oil
* Yu-Jiun Lin et al. EnergyFuels, in preparation 2015

## Slide 21
*Oilfield review, Summer 2007
Flow Assurance
The ability to produce multiphase fluids from reservoirs to processing plants in an economically and technically feasible way.
Main Technical Areas :
Prediction (Deposition Potential) --- Simulation
Prevention (Monitoring and Control) --- Sensor
Inhibition (Chemical treatment) --- Chemicals
Remediation (Recovery and Removal) --- Chemicals and mechanical force

## Slide 22
*Jill Buckley’s Lab (New Mexico Tech)
Crude Oil Components : SARA
*S. R. Panuganti et al., Fluid Phase Equilibria ,359, 2013
Notes: Asphaltene is a planar molecule with aromatic rings in the center and aliphatic chains on the sides, and there are some heteroatoms embedded such as N, O, and metal

## Slide 23
*F. M. Vargas et al, Fuel, 2013
Asphaltene Phase Behavior
Asphaltene Precipitation Envelope
Reservoir
AOP: Asphaltene Onset Pressure
Temperature and pressure can alter phase behavior of asphaltenes. Solvents can also be used to control asphaltene precipitation.
Bubble point
AOP
Notes: This is asphaltene precipitation envelope
As you can see, x-axis y-axis
Red line is AOP
Green line is bubble pt
Follow the oil production process, the oil will transport from reservoir to the surface, and the pressure and temperature will decrease.
It is like the black arrow in the left picture

## Slide 24
*O. C. Mullins et al, Energy Fuels, 2012
Yen-Mullins Model
Asphaltene Stages
P, T, or {X} changes
(Dissolved phase)
(Precipitated phase)
Sub-microaggregate
*Vargas, F. M. et al., Energy Fuels, 2010
*Jill S. Buckley, Energy Fuels, 2012
Colloidal Science
(Aggregated phase)
Notes: As you can see, this picture is Yen-Mullins Model, it describes hierarchy of the asphaltene
First, in dissolved phase, asphaltenes will be molecules, nanoaggregates, and clusters.
nanoaggregates with aggregation number of 6, and cluster with number of 8.
If PTX changed, asphaltenes will turn into precipitated phase and form sub-microaggregates, from here colloidal science comes in.
There will be two ways after precipitation, one is deposition, another is aggregation.
If the size of asphaltene aggregates are above a critical value, these aggregates will flow passing by the surface without depositing

## Slide 25
*O. C. Mullins et al, Energy Fuels, 2012
Asphaltene Stages
*Vargas, F. M. et al., Energy Fuels, 2010
*Jill S. Buckley, Energy Fuels, 2012
Deposited phase mainly from diffusion
(Aggregated phase)
Flowing-through phase by inertia
Critical size?
Arterial Deposition
Deposited phase in porous media
(from particle filtration theory)
-- First one to apply fibrous filtration theory on asphaltene deposition in porous micromodel
Inertial impaction
Interception
Brownian diffusion
Sedimentation
Electrostatic attraction
Notes: If the size of asphaltene aggregates are above a critical value, these aggregates will flow passing by the surface without depositing

## Slide 26
Understanding Asphaltene Precipitation and Deposition
Asphaltene aggregates that precipitate and deposit onto surfaces lead to plugging problems
Precipitated asphaltene aggregates that are able to flow do not pose major problems in flow assurance
*Vargas, F. M. et al., Energy Fuels, 2010
*Jill S. Buckley, Energy Fuels, 2012
Precipitation
Deposition
Notes: An asphaltene problem occurs in a two-step process: (1) precipitation of asphaltene from the reservoir fluid, which can be estimated by thermodynamic modeling and (2) deposition of the precipitated particles onto the surfaces, which ultimately results in plugging and formation damage.
Asphaltene precipitation is a necessary but not sufficient condition for deposition to take place.
Deposition depends on a number of factors, such as surface characteristics, phase behavior, rheology and fluid flow patterns.

## Slide 27
Experimental Setup
Assumptions :
Precipitation is completed in T-junction.
Deposition is the major reaction in the microchannel.
(Aggregation + Deposition) becomes (Aggregation -> Deposition)
Syringe pump
Inverted microscope
Micro-channel
T-junction
Pressure
transducer
Precipitant
Crude oil
Vial

## Slide 28
Lab on a chip (mixing, heating, separation, reaction)
Reduced reagent consumption
Faster analysis and response times due to short diffusion distances
Large surface to volume ratio of small components facilitates rapid heat transfer
Microfluidic Device
*J. Kim et al. Lab on a chip, 2012
Example: Particle sorting
Zone A: target 15 μm
Zone B: target 6 μm
Zone C: target 3 μm
Force: magnetic force or gravity
1mm

## Slide 29
*J. Wang et al, J. Disp. Sci. &Tech., 2004
*E. S. Boek et al, Energy&Fuels, 2008
50μm
500μm
Glass capillary tube -> not easy to design a complex pattern
Stainless steel -> not transparent
PDMS -> not organic resistant
Use transparent, organic resistant, and porous media design -> NOA 81
*K. Ma et al, Soft Matter, 2012
Previous Work in Microchannel

## Slide 30
n-C7 70%, Oil 30%
23 oC
Flow rate : 60 μl/min
125μm
Real-time Asphaltene Deposition
22μm
Flow direction
Notes: Reduce the porosity and permeability

## Slide 31
Characterization of Micromodel
Hydrophilic surface
Laminar flow
Empty space in the porous media
Convection-driven
Contact angle | 79.5º±2.67
Reynolds number, Re | 1.01
Initial permeability, k (Darcy) | 5.23
Porosity, | 74.79%
Pore volume | 0.124µl
Pore throat | 20µm×125µm
Péclet number for particles, | 105 - 108
Contact angle | 79.5º±2.67
Reynolds number, Re | 1.01
Initial permeability, k (Darcy) | 5.23
 | 74.79%
Pore volume | 0.124µl
Pore throat | 20µm×125µm
 | 105 - 108
Permeability is the property of rocks that is an indication of the ability for fluids (gas or liquid) to flow through rocks.

## Slide 32
Aggregation: Radius of Gyration
Volume fraction of n-heptane (vol%) | Radius of gyration, (µm)
40 | 0.9105
45 | 0.9105
50 | 0.9105
55 | 13.557
60 | 30.040
65 | 31.718
70 | 49.776
80 | 59.508
Volume fraction of n-heptane (vol%) | 
40 | 0.9105
45 | 0.9105
50 | 0.9105
55 | 13.557
60 | 30.040
65 | 31.718
70 | 49.776
80 | 59.508

## Slide 33
Precipitation and Deposition
Circle : precipitates
Rectangle : deposits
Flowing
Flow stopped
Deposits form under flowing.
When flow is stopped, asphaltenes precipitate. If the flow is restarted, these precipitates are removed. However, deposits remain.

## Slide 34
Deposition per Pore Volume
Bridging
Pore volume : empty space in the porous media
Slope will be the deposition rate (μm2/PVmix)

## Slide 35
Deposition Rate
Four Stages:
0 – 40 vol% : no deposition is detected due to two reasons :
1. only small amounts of particles exist
2. particles are so small that they are carried through by fluids
40 – 55 vol% : increase for increasing number of effective particles
55 – 65 vol% : micro-aggregates start to form, the number of effective
particles decreases -> lower chance to stick to surfaces
65 – 80 vol% : increase for bridging
Effective particle : particle with chances to stick to surfaces

## Slide 37
Deposition per Pore Volume

## Slide 38
Washing Effect
By poor solvent (2:1 heptane : toluene), some asphaltenes are removed, and a more compact deposit forms.
Good solvent
(1:1 heptane : toluene)
Poor solvent
(2:1 heptane : toluene)

## Slide 39
Indirect Method
Chart: Indirect Method
| 0 | 10.201535824436087 | 19.922682851002246 | 29.981752935193285 | 39.736310094010896 | 49.847303790710029 | 59.871999084488777 | 69.982600725935924 | 79.833055593088091 | 89.686141342632467
No inh | 4.3938 | 4.3764 | 4.4138 | 4.3706 | 4.4088 | 3.9586 | 2.9248 | 1.8284 | 1.127 | 0.53853
with inh 8 | 4.3297 | 4.266 | 4.348 | 4.2613 | 4.3834 | 3.9966 | 3.1142 | 1.8654 | 1.1818 | 0.47764
with inh 15 | 4.4318 | 4.3379 | 4.3568 | 4.3165 | 4.1728 | 3.0659 | 2.0387 | 1.1494 | 0.86857

## Slide 40
Chart: n-C7 vol%
| 0 | 10.201535824436087 | 19.922682851002246 | 29.981752935193285 | 39.736310094010896 | 49.847303790710029 | 59.871999084488777 | 69.982600725935924 | 79.833055593088091 | 89.686141342632467
No Inhibitor | 0 | 0 | 0 | 0 | 0 | 7.2033 | 31.4371 | 57.1403 | 73.5823 | 87.376
C8 Phenol | 0 | 0 | 0 | 0 | 0 | 4.1555 | 27.165 | 56.9941 | 77.6562 | 91.0973
C12 Phenol | 0 | 0 | 0 | 0 | 0 | 4.6573 | 26.1365 | 60.7012 | 75.5916 | 89.9406
Indirect Method

## Slide 41
Results of direct spectroscopy for 0.5 wt% C5+ asphaltene in toluene diluted with n-heptane and aged for 10 minutes. Inhibitor acts at high concentration of n-C7 and breaks asphaltene aggregates.
Direct Method
Smaller aggregates show less scattering

## Slide 42
Macroscale - Deposition Rate
Chart: 
* Yu-Jiun Lin et al. EnergyFuel, in preparation 2015
By mixing n-heptane with model oil, aggregates will change into three phases (spherical, fractal, chunk), and these aggregates will change behaviors of deposition.

## Slide 43
Bulk - Permeability Reduction
* Yu-Jiun Lin et al. Lab on a Chip, in preparation 2015
By applying Darcy’s law with measured pressure drop, the permeability reduction curves are obtained, and permeability is impaired significantly by asphaltene deposition.